## Slide 1: PRODUCT GUIDE
LUS-170
UV-LED Flexible ink
30-11-2017
V0.1EU
The information in this document is subject to change without notice.

## Slide 2: LUS-170 LED-UV ink
Newly developed environmentally friendly LED curable UV ink
Creating more special effects with LUS-170
  Specially developed for 4-layer print, such as Day&Nigh effect
Stretchable up to 170%
Low VOC, Nickel free
GREENGUARD Gold certified
High color density
High scratch and chemical resistance
  High scratch resistance of LUS-170 allows printing on media such as tarpaulin without need for lamination after printing
Available in 8 different colors: Cyan, Magenta, Yellow, Black, Light cyan, Light magenta, White and Clear

## Slide 3: Ink pack details
Part No. | Description | Volume | Packaging | Applicable printer |  | Shelf lifetime
LUS17-C-BA-1 | LUS-170 UV Curing Ink Cyan | 1L | Bottle | UCJV150-160 | UCJV300-75/107/160 | 12 months after production date
LUS17-M-BA-1 | LUS-170 UV Curing Ink Magenta |  |  |  |  | 
LUS17-Y-BA-1 | LUS-170 UV Curing Ink Yellow |  |  |  |  | 
LUS17-K-BA-1 | LUS-170 UV Curing Ink Black |  |  |  |  | 
LUS17-LC-BA-1 | LUS-170 UV Curing Ink Light Cyan |  |  |  |  | 
LUS17-LM-BA-1 | LUS-170 UV Curing Ink Light Magenta |  |  |  |  | 
LUS17-W-BA-1 | LUS-170 UV Curing Ink White |  |  |  |  | 
LUS17-Cl-BA-1 | LUS-170 UV Curing Ink Clear |  |  |  |  | 
Ink label
Ink pack

## Slide 4: LUS-170 LED-UV ink: Color Gamut
 | LUS-170 | LUS-200
Colors |  | 
Features | Stretchable up to 170% Flexible enough to fold Ink film is less likely to crack by folding or cutting Good media compatibility GREENGUARD GOLD certified ink Avery ICS warranty Program | Stretchable up to 200% Ink film is less likely to crack by folding or cutting High outdoor durability 3M™ MCS™ Warranty guarantees up to 6-year outdoor durability
Applications | Indoor signage and outdoor signage Printing on the material which requires post processing such as cutting or heating | Outdoor vinyl signage* Vehicle wrapping
W
K
Y
M
CC
C
W
Lm
Lc
K
Y
M
CC
C
Chart: 
| -0.9 | 59 | 67.91 | 27.24 | -33.340000000000003 | -75.77 | -0.9 | -8.59 | 54.03 | 61.93 | 15.04 | -35.36 | -60.08 | -8.59 | -4.6399999999999997 | 51.14 | 58.84 | 17.690000000000001 | -34.799999999999997 | -64.87 | -4.6399999999999997
LUS-170_4C | 85.13 | 34.47 | -11.47 | -47.5 | -38.84 | 30.62 | 85.13
LUS-200_4C | 87.69 | 35.95 | -12.11 | -37.45 | -38.36 | 26.5 | 87.69
SS21 | 100.35 | 50.79 | -17.76 | -51.74 | -47.84 | 36.74 | 100.35
Y
G
C
B
M
R
LUS-170
Ink Set: CMYK
Model: UCJV300-160
Print Mode: 600x600, 16P
Ink Limit: OFF
Color matching: OFF
Material: SPC-706
LUS-200
Ink Set: CMYK
Model: UCJV300-160
Print Mode: 600x600, 8P
Ink Limit: OFF
Color matching: OFF
Material: SPC-706
* LUS-200 is not suitable to print on tarpaulin and banner material
Measurement condition:
Cl

## Slide 5: Outdoor durability
Data
RIP Software
Mimaki: RasterLink 6 plus
HP, Epson: ONYX
Roland: Versaworks Dual
Media: PWS-G(PVC)
Test condition: Outdoor durability condition: ISO11341-1
Irradiation: 60 W/M2 consistently
Black panel temperature: 65°C
Examination tank temperature: 38°C
Relative humidity: -70%
Shower: 18 min every 2h
The durability of LUS-170 Yellow is slightly less because it is nickel-free ink
The solvent resistance of LUS-170 is less because of its flexibility. Ink comes off by scratching with liquid, Ethanol 30%
With the post processing by screen printing (solvent) varnish, LUS-170 ink layer may dissolve
The use of solvent and adhesive agent on the material printed by LUS-170 is not recommended
Please test beforehand applications which require solvent resistance

## Slide 6: Scratch resistance
Superior scratch resistance compared to solvent or latex print technologies
 | Mimaki LUS170 | HP HP 831 | Roland TrueVIS | EPSON GS3
Scratch resistance evaluation test | Excellent | Acceptable | Acceptable | NG
Test method:
Machine: Scratchiness tester RT-300
Scratchiness Paper : Sand Paper #400
Scratching time: 10 front-back motion
Media: Hiraoka SJT-V200F (Banner)

## Slide 7: Certificates
GREENGUARD Gold Certification for LED-UV inks
  Mimaki LED-UV ink LUS-170 is GREENGUARD GOLD certified.
  Products that are GREENGUARD GOLD certified meets the rigorous standards for low emission of volatile organic compounds (VOCs) and ensures that a product is acceptable for use in environments such as schools and healthcare facilities.
ICS Performance Guarantee
  The ICS Performance Guarantee assures the performance of Avery films with a printing platforms when customers are working according to the relevant Avery Dennison Technical Bulletins associated with that product

## Slide 8: Thank you
MIMAKI EUROPE B.V.

## Slide 9: Revision history
Version | Date | Content | Drafter
0.1EU | 30-11-2017 | Draft | Product Management EMEA
0.2EU | 17-10-2018 | Draft | Product Management EMEA
Do not disclose this page